## Slide 1
جوشکاری و اتصال مواد
Welding and Joining of Materials
بخش اول: فرایندها
بخش دوم: متالورژی جوشکاری

## Slide 2: Fusion Welding Processes
Fusion welding is a joining process that uses fusion of the base metal to make the weld. The three major types of fusion welding processes are as follows:
1. Arc welding:
Shielded metal arc welding (SMAW)
Flux-cored arc welding (FCAW)
Submerged arc welding (SAW)
Electroslag welding (ESW)
Gas–tungsten arc welding (GTAW)
Gas–metal arc welding (GMAW)
Plasma arc welding (PAW)
2. Resistance Welding
3. Gas welding
Oxyacetylene welding (OAW)
3. High-energy beam welding:
Electron beam welding (EBW)
Laser beam welding (LBW)
Flux-shielded Arc Welding
Gas-shielded Arc Welding

## Slide 3: Arc Welding

## Slide 4: Manual Metal Arc Welding (MMA) Shielded metal arc welding (SMAW)

## Slide 9
Butt joint
Edge joint
Corner joint
Lap joint
T joint

## Slide 12: continuous coated electrode arc welding جوشکاری قوس الکترود روپوش دار پیوسته

## Slide 13
Flux-Cored Arc Welding (FCAW)

## Slide 14
Submerged Arc Welding (SAW)

## Slide 15
Submerged Arc Welding (SAW)-Strip Electrode

## Slide 16
Submerged Arc Welding (SAW)

## Slide 17
Submerged Arc Welding (SAW)

## Slide 18
Submerged Arc Welding (SAW)
“tandem” operation

## Slide 19
Electroslag Welding (ESW)
joins metals by heating them with a pool of molten slag held between the metals and continuously feeding a filler wire electrode into it

## Slide 20
Figure 11.38 Effect of weld depth–width ratio on centerline cracking: (a) ratio too high; (b) ratio correct
Figure 11.23 centerline cracking in a coarse-grain 310 stainless steel weld
Electroslag Welding (ESW)

## Slide 21
Electroslag Welding (ESW)

## Slide 22
Gas Tungsten Arc Welding (GTAW)
Tungsten Inert Gas Welding (TIG)

## Slide 23
Gas Tungsten Arc Welding (GTAW)
Tungsten Inert Gas Welding (TIG)

## Slide 24
Gas Tungsten Arc Welding (GTAW)
Tungsten Inert Gas Welding (TIG)
DCSP/DCEN

## Slide 25
Gas Tungsten Arc Welding (GTAW)
Tungsten Inert Gas Welding (TIG)

## Slide 26
Gas Tungsten Arc Welding (GTAW)
Tungsten Inert Gas Welding (TIG)

## Slide 27
Gas Tungsten Arc Welding (GTAW)
Tungsten Inert Gas Welding (TIG)

## Slide 28: AWS Standard
سیم جوش های مورد استفاده برای مس و آلیاژهای مس A5.7
سیم جوش های مورد استفاده برای فولادهای کرم دار و کرم نیکل دار مقاوم به خوردگی A5.9
سیم جوش های مورد استفاده برای آلومینیوم و آلیاژ آلومینیوم A5.10
سیم جوش های مورد استفاده برای عملیات سطحی A5.13
سیم جوش های مورد استفاده برای نیکل و آلیاژهای نیکل A5.14
سیم جوش های مورد استفاده برای تیتانیوم و آلیاژهای تیتانیوم A5.16
سیم جوش های مورد استفاده برای فولادهای کربنی A5.18
سیم جوش های مورد استفاده برای آلیاژهای منیزیم A5.19
سیم جوش های مورد استفاده برای آلیاژهای زیرکونیم A5.24
Gas Tungsten Arc Welding (GTAW)
Tungsten Inert Gas Welding (TIG)

## Slide 29
Gas Metal Arc Welding (GMAW)
Metal Inert Gas (MIG), Metal Active Gas (MAG)

## Slide 30
Gas Metal Arc Welding (GMAW)
Metal Inert Gas (MIG), Metal Active Gas (MAG)
globular transfer
spray transfer
180 A
220 A

## Slide 31
Gas Metal Arc Welding (GMAW)
Metal Inert Gas (MIG), Metal Active Gas (MAG)
انتقال مداربسته

## Slide 32
Gas Metal Arc Welding (GMAW)
Metal Inert Gas (MIG), Metal Active Gas (MAG)
ریزش شدید
دفع کردنی
اسپری
گلوله ای

## Slide 33
Gas Metal Arc Welding (GMAW)
Metal Inert Gas (MIG), Metal Active Gas (MAG)
Ar
Ar+He

## Slide 34
Plasma Arc Welding (PAW)

## Slide 35
Plasma Arc Welding (PAW)

## Slide 36
Plasma Arc Welding (PAW)
جوش سوراخ کلیدی

## Slide 37
Arc Stud Welding

## Slide 39: Resistance Welding

## Slide 40
Resistance Welding

## Slide 41
Resistance Welding

## Slide 42
Resistance Spot Welding

## Slide 43
Resistance Spot Welding
با افزایش دما، مقاومت الکتریکی فلزات افزایش می یابد.

## Slide 44
Resistance Spot Welding
شکل های مختلف الکترود در جوشکاری مقاومتی نقطه ای

## Slide 45
Resistance Spot Welding
اتصال ورق نازک به ضخیم:
ورق ضخیم طول بیشتر (l) و مقاومت بالاتری داشته و درنتیجه حرارتی بیشتری در آن تولید می شود.
با افزایش سطح مقطع الکترود (A) مقدار R در دو ورق برابر شده و دو ورق به یک اندازه گرم می شوند.
با استفاده از الکترود با مقاومت بیشتردر سمت ورق نازک هم می توان این مشکل را کاهش داد

## Slide 46
Resistance Welding

## Slide 47
Resistance Spot Welding
در جوشکاری نقطه ای معمولا باید به دو سمت قطعه دسترسی داشته باشیم، اما می توان از تکنیک جوش سری نیز استفاده کرد

## Slide 48
Resistance Spot Welding

## Slide 49
Resistance Projection Welding

## Slide 50
Resistance Seam Welding

## Slide 51
High Frequency Resistance Welding
جوشکاری مقاومتی با فرکانس بالا: عبور جریان الکتریکی فرکانس بالا (kHz 450) توسط دو کفشک و در نتیجه تولید لایه نازک مذاب در محل تماس دو لبه

## Slide 52
High Frequency Induction Welding
جوشکاری فرکانس بالای القایی (غیر تماسی): القای جریان توسط حلقه سیم پیچ

## Slide 53
Resistance Welding
جوشکاری نقطه ای
جوشکاری نواری
جوشکاری پیش طرحی

## Slide 54: Thermo-Chemical Welding

## Slide 55
Oxyacetylene Welding
O2
C2H2

## Slide 56
Oxyacetylene Welding

## Slide 57
Oxyacetylene Welding

## Slide 58
Oxyacetylene Welding

## Slide 59
Oxyacetylene Welding

## Slide 60
Oxyacetylene Welding

## Slide 61
Oxyacetylene Welding

## Slide 62
Thermit Welding